## Slide 1: Unraveling the Origin of Coherent Helicity-Dependent Spin-Phonon Oscillations in the van der Waals Ferromagnet CrI3
Min-Cheol Lee,1 Prashant Padmanabhan,1 Mariana Fazio,2 Finn L. Buessen,3 R. Tutchton,1 Kevin W. C. Kwock,1 Sam Gilinsky,1 Sandra Biedron,2 Michael A. McGuire,4 Srinivasa R. Singamaneni,5 Dmitry A. Yarotski,1 Antoinette J. Taylor,1 Arun Paremekanti,3 Jian-Xin Zhu,1 and Rohit P. Prasankumar1
1Center for Integrated Nanotechnologies, Los Alamos National Laboratory
2 ECE Department, University of New Mexico
3 Department of Physics, University of Toronto
4 Materials Science and Technology Division, Oak Ridge National Laboratory
5 Department of Physics, University of Texas at El Paso

## Slide 2: Outline
Overview of magnetic 2D nanomaterials
  Properties of the ferromagnetic (FM) van der Waals (vdW) crystal CrI3
Revealing coherent helicity-dependent spin-phonon oscillations in bulk CrI3
Using ultrafast electron diffraction (UED) to reveal the origin of helicity-dependent oscillations in CrI3
Future plans

## Slide 3: Magnetic 2D Nanomaterials
Two-dimensional (2D) transition metal dichalcogenides (TMDs) have attracted a great deal of attention over the past decade
  Layer-dependent optical and electronic properties, including a direct bandgap when thinned down to a single atomic layer
  2D magnetic crystals such as CrI3 and Cr2Ge2Te6 exhibit ferromagnetic (FM) or antiferromagnetic (AFM) order along with both semiconducting and metallic behavior (C. Gong and X. Zhang, Science (2019); K. S. Burch et al, Nature (2018))
  Static optical measurements have shed light on their properties
C. Gong and X. Zhang, Science (2019)
MOKE and PL on monolayer CrI3
B. Huang et al, Nature (2017) ; K. Seyler et al, Nature Phys. (2018)
Ultrafast FM exchange enhancement in CrSiTe3
A. Ron et al, Phys. Rev. Lett. (2020)
Relatively few ultrafast optical experiments have been done on these novel 2D magnets, providing an exciting opportunity to learn more about their properties!

## Slide 4: CrI3 at a Glance
Van der Waals semiconductor with 1.2 eV optical gap
Rare example of a material hosting magnetic order from the bulk to the monolayer limit
Bulk and odd number of layers are ferromagnetic, bilayers are antiferromagnetic
  Intimate coupling between structure and magnetic order yields unusual phenomena
  FM magnetization along c-axis
Nonreciprocal second harmonic generation (SHG) due to time and inversion symmetry breaking in bilayers
Little known about the coupling between spin and lattice degrees of freedom on ultrafast timescales or under non-equilibrium conditions
M. A. McGuire, et al., Chemistry of Materials 27, 612 (2015)
B. Huang, et al., Nature 546, 270 (2017)
Z. Sun, et al., Nature 572, 297 (2019)

## Slide 5: Time-Resolved Polarization Rotation Microscopy
Pump
Probe
M
Magneto-optical Kerr effect

## Slide 6: Magnetization Dynamics in Bulk CrI3
RCP Pump
Time-resolved polarization rotation at 800 nm
Significant change in incoherent dynamics above and below TC = 61 K
Signal switches polarity with pump helicity
Strong coherent oscillations at THz frequencies
coherent oscillations
RCP Pump
RCP Pump
P. Padmanabhan et al., https://arxiv.org/abs/2010.04915
Notes: Polar MOKE is sensitive to out-of-plane magnetization

## Slide 7: Long-Time Dynamics in the FM Phase
                Initial rapid picosecond (ps) demagnetization
Slower demagnetization occurs on a ∼100 ps timescale
Coherent strain wave due to impulsive heating
Why do we see two-step (type-II) demagnetization dynamics?
Can we model these dynamics?
T = 15 K

## Slide 8: Modeling Demagnetization with the Microscopic Three-Temperature Model
Strong spin-orbit coupling allows for demagnetization that can be driven by Elliott-Yafet scattering and modeled with the M3TM
B. Koopmans et al., Nature Mater. 9, 259 (2010)
Notes: R is a material-specific scaling factor for the demag rate and depends on a_sf, the probability that an electron spin-flips after emission/absorption of a phonon
Type-II demag: initial rapid demag on left due to spin-flip scattering, slower e-ph coupling on middle figure, but if initial demag isn’t completed during e-ph thermalization, then the rate gets slower since the system temperature is lower after e-ph equilibration

## Slide 9: A Closer Look at the Coherent Modes
Coherent oscillations correspond to A1g symmetry phonon modes
What happens if we change the pump polarization?
L. Webster, et al., Phys. Chem. Chem. Phys. 20, 23546 (2018)
c-axis iodine atom oscillations
(~ 3.9 THz)
ab-plane iodine atom oscillations
(~ 2.4 THz)
Notes: Relatively small c-axis distortions, not necessarily lattice constant, pm (hundredths of an angstrom), time-dependent modulations of the Iodine octahedra
Why do we show the 75 K data vs. 15 K here?

## Slide 10: Pump Helicity Dependence of Coherent Modes
Above Tc, nearly equivalent amplitude for both modes under RCP and LCP pumping
Below Tc, higher energy mode has substantially lower amplitude under LCP pumping
P. Padmanabhan et al., https://arxiv.org/abs/2010.04915

## Slide 11: Mode Amplitude vs. Temperature
LCP vs. RCP intensity ratio shows sharp increase across Tc
  Demonstrates that the oscillatory amplitude is linked to underlying magnetic order, likely due to strong spin-phonon coupling
No significant change in mode across Tc
Can the phonon modulate spin exchange coupling?
P. Padmanabhan et al., https://arxiv.org/abs/2010.04915

## Slide 12: Capturing Spin-Phonon Coupling in CrI3
Model Equations
Our results demonstrate that the mode is strongly coupled to magnetic order, while the mode is not coupled at all, but the reasons for this discrepancy remain unclear. Can we gain more insight by directly measuring the atomic motions associated with both modes after polarized femtosecond optical excitation?
Notes: Pump pulse provides a helicity-dependent lattice distortion, Q=Q+psi1(1+sig*psi2*m), where Q is lattice displacement
Last term in Hamiltonian is off-diagonal symmetric exchange
Note that we could neglect coupling to other exchange terms besides J_H
DFT says that changes in Q change E by 3.2 meV/nm of displacement for A_1g(2) phonon

## Slide 13: Proposed Ultrafast Electron Diffraction Experiments on CrI3
CrI3
Optical pump
(800 nm; 1.55 eV)
Electron
probe
H ll c

## Slide 14: Using UED to Study Coherent Phonons in Quantum Materials
THz pump, UED probe experiments were performed at SLAC on the Weyl semimetal WTe2
Temporally resolved dynamics at Bragg peaks
Observed coherent acoustic phonon oscillations due to a shear mode, which drives a topologically distinct metastable state
Nature 565, 61 (2019)

## Slide 15: Using Bragg Diffraction to Probe the A1g Modes in CrI3
MeV-UED is more beneficial than time-resolved X-ray diffraction for studying lattice dynamics, due to its high spatial resolution (< 0.5 Å)
A1g2
A1g1
in-plane mode
(79 cm-1)
out-of-plane mode
(129 cm-1)
Q = (0 0 9)
Simulating changes in X-ray Bragg diffraction peaks
+
-
X-ray diffraction intensity (a. u.)
Q = (-6 8 4)
+
by a lattice modulation of ~ ±1 pm
Notes: Presumably the (-6 8 4) peak corresponds to the A1g(1) mode, and the (009) peak corresponds to the A1g(2) mode?

## Slide 16: Phonon and Magnon Dispersion of CrI3
With its ability to probe large momentum transfers (~ 10 Å-1), MeV-UED will also enable us to investigate magnons with energies similar to the A1g phonons, providing additional insight into the specific magnons that couple to the phonon in this system
Magnon dispersion
Nat. Commun. 9, 5122 (2018)
Inelastic neutron scattering
Phys. Rev. X 8, 041028 (2018)

## Slide 17: Special Equipment Requirements and Hazards
Special equipment:
None.
Hazards:
Potential hazards include the laser of the MUED instrument and the cryogenic system necessary to cool the samples to the desired temperatures (<60 K). We would also like to apply an external magnetic field up to 1 T if possible. We will work with our BNL collaborators to exercise the necessary precautions.

## Slide 18: Experimental Time Request
CY2021 Time Request
Capability | Setup Hours | Running Hours
UED Facility | 16 | 32
Time Estimate for Remaining Years of Experiment (including CY2021)
Capability | Setup Hours | Running Hours
UED Facility | 32 | 80

## Slide 19: Conclusions and Future Directions
Ultrafast optical microscopy revealed strong helicity-dependent coherent phonon oscillations in bulk CrI3
Pump helicity dependence of higher energy A1g phonon below Tc demonstrates its strong coupling to the magnetization, while lower energy A1g phonon has no measurable coupling
MeV-ultrafast electron diffraction can provide new insight into spin-phonon coupling in CrI3:
By directly resolving the relevant atomic motions for both phonon modes as a function of temperature and pump polarization, we can shed light on the differences in coupling between both phonon modes
We can take advantage of the ability of MeV-UED to track magnon dynamics, enabling us to determine the coupling of specific magnons to specific phonons
We plan to extend these studies to few-layer CrI3, providing even more insight into this hotly studied material
P. Padmanabhan et al., https://arxiv.org/abs/2010.04915

## Slide 20: Layer-Dependent Magnetic Properties of CrI3
An external magnetic field (~1 T) can switch the 2D magnetism of vdW CrI3.
Bulk:
Ferromagnetic (TC = 61 K)
c
Monolayer:
Ferromagnetic
(TC = 45 K)
M
c
c
Bilayer:
Antiferromagnetic
(TN = 61 K)
Magneto-Optical Kerr effect
Nature 546, 270 (2017).

## Slide 21: Excitation and Coupling to Spin System
I. Lee, et al., Phys. Rev. Lett. 124, 017201 (2020)