## Slide 1: HySpec: new spectrometer is hosting users and preparing for polarization analysis
Barry Winna, Uwe Filgesb, V. Ovidiu Garleaa, Melissa Graves-Brooka, Mark Hagena,c, Peter Jianga, Michel Kenzelmannb, Larry Passelld, Stephen M. Shapirod, Xin Tonga, Igor Zaliznyakd
a Oak Ridge National Laboratory
b Paul Scherrer Institut
c European Spallation Source
d Brookhaven National Laboratory,
1 RSI 85, 045113 (2014)
2 PRB 89, 144417 (2014)
3 PRL 112, 187202 (2014)
4 O Delaire et al in prep
5 M Lumsden et al in prep
 | User
 | Experiments
Spring 2013 | 6
Fall 2013 | 17
Spring 2014 | 16
the high-flux, coarse energy resolution, cold neutron choice among SNS direct geometry spectrometers1
HOPG
vertical focusing
Heusler vertical focusing and polarizing
 | (m)
L1 | 37.2
L2 | 3.6
L2* | 1.8
L3 | 4.5
At its core, a Direct Geometry Spectrometer..
..using features of a Triple Axis Spectrometer:
Chart: Incident energy (meV)
-Vertical Bragg focusing
-Variable final flight path
 | (deg)
Horizontal Acceptance | 60
Vertical Acceptance | 15
Vertical Divergence* | 4.7
Polarization Analyzer option 1: 3He Analyzer Cell Spin-Exchange Optically Pumped
Polarization Analyzer Option 2: Polarizing Supermirror array
Intensity at 15 meV, 180 Hz | 4.20E+05
(n/s/cm^2/MW) | 
Elastic Resolution (FWHM) | 2-5% Ei
Incident Energy Range (meV) | 3.8-50
Fermi chopper,
30-420 Hz
Incident beam flipping ratio | 
at 15 meV | 
with Mezei flipper | 23
with high Tc cryo flipper6 | 32
Y0.7Lu0.3MnO3 at 4K: dotted lines show calculated spin wave dispersion with magnetoelectric coupling in this multiferroic2
Fe1.09(1)Te: symmetry forbidden (1,0,0) & (0,1,0) reflections below ~60 K reveal presence of bond-order wave transition, suggesting ferro-orbital coupling3
K2V3O8: Spin waves in
S=1/2 square lattice
antiferromagnet5
KTa0.88Nb0.12O3:
TO branch softening4
Drop-in analyzer cell commissioning with neutrons, NIST banana cell and RF flipping
Aberration-corrected coils centered on sample, uniformity to 3E-5 cm-1
SEOP station attached to detector vessel, with mechanical transfer of polarized gas to optimum shape quartz wide-angle cell7
Status: all parts delivered, assembly and offline testing underway
Status: Remanent field array ready to ship from PSI. Magnetizer delivered and tested at HYSPEC.
6 T. Wang et al, accepted, IOP, Neutron optics & Detectors
7 RSI 84, 065108 (2013)
8 http://dx.doi.org/10.5286/SOFTWARE/MANTID
9 J. Tranquada et al; acquired May 2014
User Program with
unpolarized neutrons
Hybrid
Spectrometer:
Commissioning and Development with
Polarized neutrons
Combining data sets at different detector vessel positions is trivial using Mantid8. La1.75Sr0.25NiO4 data measured9 at detector angle ranges 5-65o and 60-120o.
Detector vessel range -30o to 30o is used to measure CrCl21