Table 3

| Table of Filter Lenses for Protection From Radiant Energy |
| --- |
| Type of Operation | Electric Size 1/32 in. | Arc Current (Amp) | Minimum Protective Shade (a) |
| Shield metal arc welding (SMAW) | Less than 3 | Less than 60 | 7 |
|  | 3 to 5 | 60 to 160 | 8 |
|  | 5 to 8 | 160 to 250 | 10 |
|  | More than 8 | 250 to 500 | 11 |
| Gas metal arc welding and flux cored arc welding (GMAW) |  | Less than 60 | 7 |
|  |  | 60 to 160 | 10 |
|  |  | 160 to 250 | 10 |
|  |  | 250 to 500 | 10 |
| Gas tungsten arc welding (GTAW) |  | Less than 50 | 8 |
|  |  | 65 to 150 | 8 |
|  |  | 150 to 500 | 10 |
| Air carbon arc cutting (CAC-A) | (light) | Less than 500 | 10 |
|  | (heavy) | 500 to 1000 | 11 |
| Plasma arc welding (PAW) |  | Less than 20 | 6 |
|  |  | 20 to 100 | 8 |
|  |  | 100 to 400 | 10 |
|  |  | 400 to 800 | 11 |
| Plasma arc cutting (PAC) | Light(b) | Less than 300 | 8 |
|  | Medium (b) | 300 to 400 | 9 |
|  | Heavy (b) | 400 to 800 | 10 |
| Torch brazing |  | NA | 3 |
| Torch soldering |  | NA | 2 |
| Carbon arc welding (CAW) |  | NA | 14 |

| Type of Operation | Plate Thickness | Minimum Protective Shade (a) |
| --- | --- | --- |
|  | Inches | Mm |  |
| Gas welding (OFW) Light | Under 1/8 | Under 3.2 | 4 |
| Medium | 1/8 to ½ | 3.2 to 12.7 | 5 |
| Heavy | Over 1/2 | Over 12.7 | 6 |
| Oxygen Cutting (OC) Light | Under 1 | Under 25 | 3 |
| Medium | 1 to 6 | 25 to 150 | 4 |
| Heavy | Over 6 | Over 150 | 5 |

Source: OSHA 29 CFR 1910.133 Personal Protective Equipment, Eye and Face Protection

(a) As a rule of thumb, start with a shade that is too dark to see the weld zone. Then, go to a lighter shade that gives a sufficient view of the weld zone without going below the minimum. In oxyfuel gas welding or cutting where the torch produces a high yellow light, it is desirable to use a filter lens that absorbs the yellow or sodium line in the visible light spectrum of the operation.

(b) These values apply where the actual arc is clearly seen. Experience has shown that lighter filters may be used when the arc is hidden by the workpiece.