## Slide 1
Hyperspectral Imaging with XRS Raman scattering
Application to Ancient Materials
Jean-Pascal Rueff
Synchrotron SOLEIL

## Slide 2: Acknowledgments
C. Sahle, A. Mirone
L. Bertrand, P. Guériau
U. Bergmann
R. Popelka-Filcoff
S. Bernard
J. Ablett, D. Céolin, D. Prieur, R. Georgiou (PhD, SOLEIL / IPANEMA)
N. Brun

## Slide 3
magnons
Dynamical structure factor S(q,w)
> Low-energy XAS
in the energy loss domain
C. Sahle et al., J. Synchrotron Rad. (2017)
XRS

## Slide 4
Compton
Elastic
graphite, 6 keV, q= 5.6 A-1
C K-edge
XRS
π*
σ*
< 1min
bulk sensitivity
q2 dependence
non-dipolar contrib.
XRS at high Q

## Slide 5
Compton
Elastic
graphite, 6 keV, q= 5.6 A-1
C K-edge
XRS
π*
σ*
< 1min
bulk sensitivity
q2 dependence
non-dipolar contrib.
XRS at high Q

## Slide 6
O K-edge in MgSiO3 under high pressure
Lee et al., PNAS (2008) 105, 7925
C K-edge in graphite under high pressure
Mao et al., Science (2003), 302 425
XRS at extreme conditions
Review in JPR and A. Shukla, Rev. Mod. Phys. (2010), 82 847

## Slide 7
XRS in ancient materials

## Slide 8
XRS in ancient materials
P. Gueriau, JPR, S. Bernard, J. A. Kaddissy, S. Goler, C. J. Sahle, D. Sokaras, R. A. Wogelius, P. L. Manning, U. Bergmann, and L. Bertrand, Analytical Chemistry (2017), 89, 10819.
U. Bergmann, R. Georgiou, P. Gueriau, JPR, L. Bertrand, Reflet de la Physique (2019) in press

## Slide 9
C-speciation by NEXAFS
J. Sedlmair et al., J Soils Sediments (2012) 12,24
D. Solomon et al., Soil Sci. Soc. Am. J. 73 (2009), 1817.

## Slide 10
HAXPES and RIXS in the 2.3 - 12 keV energy range
DCM (Si 111) and HRM (dE = 100 meV - 1 eV)
spot size : 30 x 80 µm2
U20 in-vacuum undulator
HAXPES station
RIXS station
spot size : 30 x 80 µm2
beamline
focusing optics
KB : 15 x 15µm2
monochromators
JPR, J. M. Ablett, D. Céolin, D. Prieur, Th. Moreno, V. Balédent, B. Lassalle, J. E. Rault, M. Simon, and A. Shukla, J. Synchrotron Rad. (2015), 22, 175.

## Slide 11
Short arm for multianalyzers setup
(0.5 - 1m radius)
Long arm
(1 - 2m radius)
sample stage
RIXS endstation

## Slide 12
4 x 1
RIXS - XES
Multi-analyzers
J. M. Ablett, D. Prieur, D. Céolin, B. Lassalle-Kaiser, B. Lebert, M. Sauvage, Th. Moreno, S. Bac, V. Balédent, A. Ovono, M. Morand, F. Gélebart, A. Shukla, and JPR, J. Synchrotron Radiation (2019), 26
2 x 2
XRS

## Slide 13
HRM
2 sets of crystals
  4 x Si(110) sym
  4 x Si(110) asym
0.1 eV < dE < 0.4 eV
@ 4 - 12 keV

## Slide 14
sample
x-ray
SDD
detector
2θ
analyzers
He bag
XRS setup

## Slide 15
R. Georgiou, R. Popelka-Filcoff et al., in prep. (2019)
C speciation in resins

## Slide 16
Lepidodendron fossil
(300 Mya)
Towards XRS imaging

## Slide 17
C K-edge
C-speciation images
2D x-rays raster scan
2D C-speciation in fossilized plant
R. Georgiou, P. Gueriau, C. Sahle, A. Mirone, S. Bernard, R. Garrouste, U. Bergmann, J.PR and L. Bertrand, Science Advances (2019), in press

## Slide 18
2D x-rays raster scan
2D
analyzer
detector
> 3D volume
depth
3D imaging
Huotari et al., Nature Materials (2011)
Direct tomography

## Slide 19
depth
spectrum
4D hyperspectral imaging
2D x-rays raster scan
2D
analyzer
detector
> 3D volume
Huotari et al., Nature Materials (2011)
Direct tomography

## Slide 20
2D detector
(beam direction)
Coll. IPANEMA, ESRF
Case study (ID20, ESRF)
isosurface energy integrated intensity
R. Georgiou, P. Gueriau, C. Sahle, A. Mirone, S. Bernard, R. Garrouste, U. Bergmann, J.PR and L. Bertrand, Science Advances (2019), in press
30 Mya (Oise, France)

## Slide 21
30 Mya (Oise, France)
isosurface energy integrated intensity
Coll. IPANEMA, ESRF
Case study (ID20, ESRF)
R. Georgiou, P. Gueriau, C. Sahle, A. Mirone, S. Bernard, R. Garrouste, U. Bergmann, J.PR and L. Bertrand, Science Advances (2019), in press

## Slide 22
amber
amber+chitin
Case study (ID20, ESRF)
Coll. IPANEMA, ESRF
decomposition using model spectra
R. Georgiou, P. Gueriau, C. Sahle, A. Mirone, S. Bernard, R. Garrouste, U. Bergmann, J.PR and L. Bertrand, Science Advances (2019), in press

## Slide 23
Coll. IPANEMA, ESRF
Case study (ID20, ESRF)
amber
amber+chitin
decomposition using model spectra
R. Georgiou, P. Gueriau, C. Sahle, A. Mirone, S. Bernard, R. Garrouste, U. Bergmann, J.PR and L. Bertrand, Science Advances (2019), in press

## Slide 24
Model free spectral unmixing
Bayesian linear unmixing
N. Dobigeon et al., Ultramicroscopy (2012), 25–34.
Coll. LPS

## Slide 25
4 analyzers
MATRIXS project
detector
sample chamber
x-ray

## Slide 26
faster XRS
hyperspectral images
15 x 15 µm2 resolution
tomography
SOLEIL Upgrade
40 analyzers
detector
x-ray
MAssive Tabular aRray for Inelastic X-ray Scattering
MATRIXS project
sample chamber

## Slide 27
40 x analyzer modules
Si(110)
MAssive Tabular aRray for Inelastic X-ray Scattering
MATRIXS project
> available in 2020 at GALAXIES
design

## Slide 28
Conclusions
Bulk sensitive low-energy XAS
  avoid surface sensitivity
  extreme conditions
Chemical Imaging / Tomography
Applications to energy / battery

## Slide 29
Thank you for your attention !

## Slide 30
    q plays the role of ε in XAS
XRS equivalence to XAS
Triakonta-
dipole
octupole
R.A. Gordon et al., EPL 81 (2008)